## Slide 1
APD simulations using Silvaco
Contribution from – Ranjit Dalal
Delhi Uni.
June 2, 2016

## Slide 2
Simulation Structure
200 Micron Thick APD (p-in-n)
Error function doping profile (very similar to measured one)
  Junction Depth = 57 micron micron
- Bulk Doping - 1.4 x 1014 cm-3 (Measured value)
Three different type of lasers
  670nm, 980nm, 1060nm Lasers
External circuit (Bias T) is implemented for transient simulation
1x1x40 µm3 device
p+
n+
~15µm of front side is not
depleted

## Slide 3
TCT Simulation for different Wavelengths
Very fast initial peak for all the laser wavelengths
  Due to drift component of current
Large (and slow) diffusion component for 670nm laser
  Almost all of the laser energy is deposited within few micron of front side
1060 nm laser is creating fastest signal
- Similar case is expected for charged particles

## Slide 4
TCT signal for 1060nm front laser (Bias vary)
Extremely fast signal with about 2-3nm width
Signal will be compared with CERN measurements
Bias Voltage vary

## Slide 5
Signal evolution (after 1 ns of laser fire)
Total Current Density
Hole component
e- component
- hole/electrons get separated within 1ns for infrared laser
- Similar evolution is expected for charged particles too

## Slide 6
Effect of Bulk doping variation
Bulk doping vary
- Significant effect of bulk doping is seen

## Slide 7
Gain vs bias for 1060nm laser (3 bulk dopings)
Significant effect of bulk doping on device gain
  Higher bulk doping results in narrow depletion region or higher electric field for a given bias
Slight different bulk doping can result in significant gain variation
Must be carefully tuned
Linear Scale
Log scale

## Slide 8
Gain vs bias for bulk 1.4x1014 cm-3
- Higher gain for 670nm, lowest for 1060nm!

## Slide 9
Gain vs bias (Simu. and measured result)
Simulation and measured values have similar trends and values
Remember, there can be slight variation in bulk doping (for different devices), different
way of calculating and measuring device gain and different baselines for gain calculating
(500V for measurement, signal without multiplication for simulation)

## Slide 10
Edge-TCT for APD
Laser used
1060nm
Laser Width = 1 µm
Position = 1µm to 170µm (5 µm step)
(Since longer Laser rise time may affect APD signal
timing profile, All simulations are carried out with 1ps laser rise time
Gain = Total collected charge (with multiplication on)/ Collected charge (with multiplication off)
APD Bulk = 1.4e14cm-3
Junction Depth = 57µm
Laser

## Slide 11: E field for different Bias
With increase in bias, Depletion region (mainly) expand in backside bulk
Should not expect much improvement with bias (for front diffusion component) !
No multiplication beyond 100 micron depth (this number depends on bias)

## Slide 12: Bias = 1600V

## Slide 13
Signal evolution near front surface eTCT positions
Very slow diffusion component
Front side can be removed with impunity

## Slide 14
Signal evolution for different eTCT positions
Slow signal for 10-15µm location (diffusion component is significant)
Highest multiplication for 20-25µm laser position
Multiplication decreases for deeper locations
No multiplication after 90µm

## Slide 15: Bias = 1700V

## Slide 16
Signal evolution for different eTCT positions
Slow signal for 10-15µm location (diffusion component is significant)
Highest multiplication for 20-25µm laser position
Multiplication decreases for deeper locations
Almost no charge multiplication below 90µm location

## Slide 17: Bias = 1800V

## Slide 18
Signal evolution for different eTCT positions
Slow signal for 10-15µm location (diffusion component is significant)
Highest multiplication for 20-25µm laser position
Multiplication decreases for deeper locations
No multiplication after 90µm

## Slide 19
eTCT Gain Variation with Bias
- APD gain is practically coming from first 70-80 µm of device
- Some of the simulation points for 1800V are yet to be come

## Slide 20: eTCT signal comparison for diff bias
15 Micron laser position
20 Micron laser position

## Slide 21: backup

## Slide 22
Gain vs bias for 670nm laser (three bulk doping)

## Slide 23
Gain vs bias for 980nm laser (3 bulk dopings)

## Slide 24
Signal evolution for different eTCT positions
2ns time window

## Slide 25
EdgeTCT gain for APD
Gain variation vs laser depth
eTCT profile for APD is very different from usual diodes
  Depend on drift and diffusion components
  Depends on multiplication