## Slide 1: RMD 8x8 mm2 APD Packaging on CERN Alumina Test Boards
B. Harrop
Princeton University
March 9, 2017

## Slide 2
Magnetron Sputtering of the Titanium/Gold Contacts

## Slide 3
Shadow Mask
Mask Removal
Back Contact
Top Contact
Magnetron Sputtering of the Titanium/Gold Contacts
(Continued)
50/200-nm Ti/Au

## Slide 4
Mounting the APD to the Substrate with Epotek H22 Silver-Loaded Epoxy
CERN Alumina Substrate
Screen, 50 m of Silver Epoxy
Remove 50-m Mask

## Slide 5
Mounting the APD to the Substrate with Epotek H22 Silver-Loaded Epoxy
(Continued)
Die Bond (Place) APD onto Silver Epoxy
Cure Silver Epoxy @ 150C, 5 minutes

## Slide 6
Ground 25-m Aluminum Wirebonded Contact
To Top Side

## Slide 7
Bond the Mesh and Wirebond to the APD
Future version will have mesh fabricated on Kapton
5-m Nickel, Au-Flashed, 50-m Kapton Mesh
Mesh is 9.5-mm square, 8/160-m pitch
Kapton is 10.2-mm square
Mounted Mesh on APD
APD is 10 mm square
Future version will have a notch
in the mesh/Kapton for
the top contact/wirebond

## Slide 8
Completed Package
Except for wirebond to top right SMA
+HV connector to bottom side
Signal connector
Thermistor
Wire bond to be added between mesh and signal pin
In this scenario, the signal readout is between the mesh and the APD top contact, rather than between the mesh and the bottom contact. As such, time walk and signal uniformity will be poor, due to the “high” resistivity of the top contact. Should instead have capacitive coupling between the signal pin and the bottom side contact.
Should add 10 M protection resistor here (after cutting the trace to create a gap for the resistor)