## Slide 1: Mesh APD signal comparison between 980nm and 670nm Laser Diode triggered pulses
C. Lu
Princeton University
(1/12/2016)

## Slide 2
Reexamination of deep defused silicon avalanche photodiode gain and quantum efficiency
Mickel McClish, et al.
IEEE Transaction on Nuclear Science, Vol. 53, No. 5, Oct. 2006
Cross-sectional view of RMD deep diffused APD.
RMD deep diffused APD structure

## Slide 3
RMD deep diffused APD structure in simulation
V
E
Cathode +HV
Anode -HV
Removed
Avalanche region,
P doping: Al
N doping: Ga

## Slide 4
Calculation of E-field in the APD
(see my report “Simulation of RMD APD with VTCAD” on 10/29/2012)
Extract the net charge distribution along with the central line of the APD model (x kept at 50 m, y from -190 m to 60 m):
Net charge distribution along with the central line (y axis direction).
According to Poisson equation, we can use numerical integration of the charge density along with y axis to get E-field:
Ey(V/cm) = 1/,  = 11.7 x 8.85 x 10-14 (F/cm),
q is the charge density (as shown on the left),
integration from -190 m to 60 m.
The maximum E-field for -1500V bias is ~189 kV/cm.
Chart: y (m)
Chart: y (m)

## Slide 5
Avalanche region in APD
To estimate the thickness of the avalanche region in APD, we assume the avalanche starts at bias -1500 V. On previous slide we have shown that at -1500 V the maximum E-field is ~ 189 kV/cm, thus we can draw a line on the right plot, estimate the thickness of the avalanche region t.
(M. McClish et al. IEEETNS 53 (2006) 1)
At -1700 V, t ~ 30 m,
-1750 V, t ~ 33.8 m,
-1800 V, t ~ 36.3 m,
-1900 V, t ~ 42.5 m.
Chart: y (m)

## Slide 6
Test mesh APD with red laser diode (670nm)
HP pulser settings: Width=1ns, Vhigh=4V, Vlow=0V, Comp=Off
Ch1=Cathode; Ch2=Mesh; Ch3=Anode; Ch4=Trigger; APD HV=-1800V

## Slide 7
Test mesh APD with red laser diode (670nm)
HP pulser settings: Width=2ns, Vhigh=4V, Vlow=0V, Comp=Off
Ch1=Cathode; Ch2=Mesh; Ch3=Anode; Ch4=Trigger

## Slide 8
Test mesh APD with red laser diode (670nm)
HP pulser settings: Width=3ns, Vhigh=4V, Vlow=0V, Comp=Off
Ch1=Cathode; Ch2=Mesh; Ch3=Anode; Ch4=Trigger

## Slide 9
Test mesh APD with red laser diode (670nm)
HP pulser settings: Width=4ns, Vhigh=4V, Vlow=0V, Comp=Off
Ch1=Cathode; Ch2=Mesh; Ch3=Anode; Ch4=Trigger

## Slide 10
Test mesh APD with infrared laser diode (980nm)
HP pulser settings: Width=0.7ns, Vhigh=3V, Vlow=0V, Comp=Off
Ch1=Cathode; Ch2=Mesh; Ch3=Anode; Ch4=Trigger; APD HV=-1800V

## Slide 11
Test mesh APD with infrared laser diode (980nm)
HP pulser settings: Width=1ns, Vhigh=3V, Vlow=0V, Comp=Off
Ch1=Cathode; Ch2=Mesh; Ch3=Anode; Ch4=Trigger; APD HV=-1800V

## Slide 12
Test mesh APD with infrared laser diode (980nm)
HP pulser settings: Width=2ns, Vhigh=3V, Vlow=0V, Comp=Off
Ch1=Cathode; Ch2=Mesh; Ch3=Anode; Ch4=Trigger; APD HV=-1700V

## Slide 13
Comparison between 670nm and 980nm
HP pulser settings: Width=2ns
Chart: 
Chart: 
The very first part of the rise edges of 670nm signal is fast, similar to 980nm signal, then followed by slower and broader signal.
Fast leading edge
Slow leading edge
Fast leading edge

## Slide 14
Comparison between 670nm and 980nm
HP pulser settings: Width=2ns
Chart: 
For anode signal we don’t see the fast leading edge, only slow rising edge!

## Slide 15
Comparison between 670nm and 980nm
The absorption coefficient of silicon (http://www.pveducation.org/pvcdrom/materials/optical-properties-of-silicon): @670nm 2380/cm, @980nm 95.9/cm.
Because the large difference the depths of the laser light created photoelectron are quite different.
T = , µ is the absorption coefficient, L is the thickness of silicon layer.
For 670nm laser light the photoelectrons are only created at the very thin layer of silicon surface, but for 980nm laser light it can penetrate deep into the entire APD active layer. The reason to cause signal shape difference might be due to this, it needs detailed simulation to confirm.