## Slide 1: New Directions in Robust Photocathodes Using the tools of materials science to engineer alkali antimonide cathodes for performance and speed
John Smedley
Brookhaven National Laboratory
Feb 21, 2017

## Slide 2: What do we want out of an electron source?
The electron beam properties determine the photon beam properties
  Pulse duration, degree of coherence, flux
In all light sources through 3rd generation, the phase space is determined by the ring
In X-ray free electron lasers (LCLS II, XFEL, MaRIE), this will change – the electron source will determine the beam properties
The highest brightness sources available are photoinjectors, which use a laser on a photocathode to control the spatial and temporal profile of the emitted electron beam

## Slide 3
What is a photocathode?
A surface that emits electrons when illuminated (Go Einstein!)
What are they used for?
Traditionally, in image intensifiers and photodetectors/PMT
Super-Kamiokande
Neutrino Detector
11,200 20”
K2CsSb PMTs

## Slide 4
What is a photocathode?
A surface that emits electrons when illuminated (Go Einstein!)
What are they used for?
Traditionally, in image intensifiers and photodetectors/PMT
More recently also as electron sources for accelerators
Allow control of the spatial and temporal profile of the beam
Produce a “Brighter” electron beam than can be achieved from other sources
What makes a good photocathode?
Quantum Efficiency, lifetime, fast temporal response
Correlation of emitted electrons (low beam “temperature”, or emittance), high current, low dark current, spin polarization
Important applications to other fields – Photovoltaics, PET imaging

## Slide 5
Unproductive absorption
In “magic window”
Onset of e-e
scattering
K2CsSb: A Good Candidate
T. Vecchione et al., Appl. Phys. Lett. 99, 034103 (2011)
Good
Lifetime
1e-9 mBar
Low transverse
Momentum (543 nm)
0.36 µm/mm

## Slide 6
Traditional Sequential Deposition of K2CsSb
High QE and Rough Surface
  S. Schubert et al., APL Materials 1, 032119 (2013)
  T. Vecchione, et al, Proc. of IPAC12, 655 (2012)
  25 nm roughness, 100 nm spatial period
  Emittance vs field measured with Momentatron, 532 nm light

## Slide 7
UHV system ( 0.2 nTorr base pressure)
Residual Gas Analyzer (RGA)
Heating/cooling substrate/cathode
Load lock
  fast exchange of substrates
  gun transfer
Horizontal deposition of Sb, K and Cs.
Sputter Deposition!
Camera 1
Camera 2
Two 2D detectors (Pilatus 100K)
In operando analysis during growth
(setup at NSLS/X21 & CHESS G3 – ISR soon)
XRF, XRD, XRR, GISAXS, QE

## Slide 8
Horizontal evaporation of three sources:
140
25
T(C)
t
Sb
K
Cs
Recipe:
100
Experimental set up: K2CsSb cathode growth
X-rays
Sb
K
Cs
FTM
P=1x10-10 mbar
QE(%)
t
K
Cs
QE during growth (532 nm laser)

## Slide 9: 165Å Sb at RT on Si(100)
Simultaneously Acquire XRD and GISAXS
Understanding reaction dynamics through crystalline phase evolution
Map the thickness and roughness evolution of the cathode
Is there a correlation between reactivity, QE and roughness?
Camera 1: GISAXS & XRR
Camera 2: WAXS
0Å
165Å
time
Sb peaks
(012)
(104)
(110)
(003)
14.9˚
39.3˚

## Slide 10
Reaction Dynamics
Antimony evaporated on Si, 0.2 Å/s; crystallize at 4nm
K deposition dissolves Sb layer - This is where roughening occurs!
QE increase corresponds with KxSb crystallization
Cs increases lattice constant and reduces defects
M. Ruiz-Osés et al., APL Mat. 2, 121101 (2014)

## Slide 11: Cathode Texture
Sb evaporated at RT
Clear [003] texture
Add Potassium at 140C
Textured final film
But not K3Sb
Add Cesium at 140C
Textured final film
Both [220] & [222]
(domains?)
Final QE 7.5% @ 532nm

## Slide 12: Engineering a Smoother Cathode
Idea: Never let Sb crystalize
Substrate: Si (100)
100 C
+3nm Sb
Sb
125 ̊C
+K until photocurrent peaks
KxSb
125 ̊C
+Cs until photocurrent peaks
CsK2Sb
2nd layer: +5nm Sb
M. Ruiz-Osés et al., APL Mat. 2, 121101 (2014)

## Slide 13: X-ray reflectometry (XRR) provides in-situ thickness monitoring
Understand ‘sticking’ coefficient of materials to substrates at various temperatures
Observe the intermixing vs layering of materials
Observe the onset of roughness
Notes: This when we have fixed layer…
For In-situ growth -> fringes disappears… there are two reasons: either it is too thick or surface becomes rough
We get interference pattern when we have constructive interference.

## Slide 14: XRR shows roughness evolution
Deposited Layers | Total Thickness (Å) | Roughness (Å)
Cs-K-Sb-Cs-K-Sb/Si | 469 | 32
K-Sb-Cs-K-Sb/Si | 449 | 36
Sb-Cs-K-Sb/Si | 200 | 21.3
Cs-K-Sb/Si | 174 | 13.2
K-Sb/Si | 141 | 10.5
Sb/Si | 35 | 2.9
Si Substrate | - | 3.1
The substrate fit includes 1.5 nm of SiO2
Multi-layer subcrystalline film is smoother,
At slight loss of QE

## Slide 15
K2CsSb
sputter gun
Sputter growth of Bi-alkali photocathode
Before
Sputtering
Sputter target and sputter gun was product of RMD. Inc. Photos of sputter target prep are contributed by H. Bhandari

## Slide 16
layer | K (±0.1) | Sb (±0.05) | Cs (±0.05) | K/Cs
K2CsSb sputter | 0.85 | 1.00 | 0.41 | 2.08
Cs | 0.84 | 1.00 | 1.75 | 0.48
25 nm K2CsSb + layers of (total 30 nm) Cs evap.
Silicon substrate at 90 C, layer barely crystalline
Sputter Growth
25 nm sputtered layer + Cs
50 nm sputtered layer + Cs
Notes: Examples of typical data set

## Slide 17
Surface roughness & QE of Sputtered Photocathodes
Peak QE > 20%
Green QE: 4.3%
 | Thickness (Å) | Roughness (Å)
3rd Cs | 416.0 | 5.67
2nd Cs | 341.3 | 4.94
1st Cs | 249.5 | 4.91
sputter K2CsSb | 234.2 | 5.17
SiO2 | 10.24 | 3.27
Substrate (Si) | --- | 3.75

## Slide 18: Software Upgrades - Real Time XRF during growth
Currently using to regulate ternary co-evap

## Slide 19
Ternary Co-evaporation Simultaneously evaporate from Sb evaporator and K,Cs effusion cells
Cs Cell
K capsule
In situ, In operado XRR, XRF, XRD & Quantum efficiency (QE) measurement
J tube
Growth rate are controlled by J tube temperature, valve and shutter

## Slide 20
(222)
(420)
(422)
(440)
Thickness
Real time
XRD
Real time
Fluorescence
QE
~10nm

## Slide 21
Stoichiometry & Structural Analysis
Camera 2
Highly textured
K2CsSb phase!
Camera 1
Grain size 20.2nm
(220)
(111)
(222)
Grain size 27.7nm
(400)
(200)
 | K | Sb | Cs
L004 Si | 2.50 | 1.00 | 1.16
L005 Si | 2.37 | 1.00 | 0.91
L006 Si | 2.21 | 1.00 | 0.95
L011 Si | 2.07 | 1.00 | 0.94
L012 MgO | 1.98 | 1.00 | 0.88
Good K/Cs/Sb ratio!

## Slide 22
 | QE@532nm(%) | Roughness(A) | Thickness (A) | Grain size (A)
L004 Si | 4.9 | 3.5 | 234 | 155
L005 Si | 5.8 | 11.5 | 815.3 | 277
L006 Si | 5.4 | 13.8 | 757.5 | 202
L011 Si (HT Si) | 6.4 | 79.0 | 905.2 | 208
L012 MgO | 5.7 | 8.6 | 566.4 | 193
Surface Roughness & QE

## Slide 23: Alkali Antimonide Cathodes What we’ve learned
We now have a tool which is capable of optimizing growth parameters for figures of merit other than Quantum Efficiency
We understand the formation chemistry of these materials, and why traditional deposition results in rough cathodes
RMS roughness down almost 2 orders of magnitude, to ~atomic scale
Avoiding crystalline Sb helps, as does co-evaporating alkali
Sputter deposition is good – easy to do, covers large area, almost atomically smooth even for thick films – but alkali poor
Real time XRF feedback provides option of ternary coevaporation, producing best cathode
Can now consider heterojunctions and doping of alkali antimonides (following a similar development path to the III-V materials)
Can consider ultra thin (under 10 nm) cathodes to improve response time
Large grain, smooth surfaces should be more resistant to ion bombardment and chemical poisoning than conventional cathodes

## Slide 24: Thanks for your attention!
Thanks to K. Attenkofer, S. Schubert, M. Ruiz Oses, J. Xie, J. Wang, H. Padmore, E. M. Muller, M. Gaowei, J. Walsh, T. Vecchione, X. Liang, J. Sinshiemer, Z. Ding
DOE Office of Science – Basic Energy Science

## Slide 25: Hot off the presses – Co-evaporation
Effusion Cell (K & Cs)
Pure metals
Antimony Crucible with cooled mask
Rates balanced with real-time XRF
QE over 30% (8% Green)
XRR oscillations
Chart: Wavelength (nm)

## Slide 26: Hot off the presses – Co-evaporation
Effusion Cell (K & Cs)
Pure metals
Antimony Crucible with cooled mask
Rates balanced with real-time XRF
QE over 30% (8% Green)
XRR oscillations
Chart: Wavelength (nm)
23 nm thick, 0.5 nm roughness

## Slide 27
Stepwise High Resolution XRD
A little bit of Potassium goes a long way…
S. Schubert et al., J. Appl. Phys. 120, 035303 (2016)
Sb
Sb
K
K

## Slide 28
Stepwise High Resolution XRD
A little bit of Potassium goes a long way…
S. Schubert et al., J. Appl. Phys. 120, 035303 (2016)
K
K
Room Temperature
Recrystallization to K3Sb
Better QE of K3Sb
Principally Hexagonal
100C Substrate
Recrystallization to KxSb
Cubic K3Sb first
Eventually Hex appears (oops!)

## Slide 29
Stepwise High Resolution XRD
S. Schubert et al., J. Appl. Phys. 120, 035303 (2016)
Cs
Cs
Room Temperature
K3Sb resists Cs incorporation
QE never improves
100C Substrate
Cubic K3Sb converts quickly
Hex K3Sb mostly converts

## Slide 30
Stepwise High Resolution XRD
S. Schubert et al., J. Appl. Phys. 120, 035303 (2016)
100C without “too much” K
15 nm Sb, 70 nm K
Stop at “mixed phase” KxSb
lower QE of K3Sb
90 nm Cs sufficient
Full conversion to CsK2Sb
QE = 6.7% at 532 nm

## Slide 31
1st Sb
2nd (K,Cs)+Sb
3rd
4th
5th
6th
XRF analysis results of co-dep sample.
→ Calculated stoichiometry shows Sb, Cs - excess, K-deficient
Substrate: MgO
~120 C
+1.5 nm Sb
Sb
~120 C
+K, Cs
CsxKySb
Repeat growth (6 layers)
Yo-yo deposition

## Slide 32: Yo-yo deposition
layer | Roughness (Å) | Thickness(Å) | QE
6th (K,Cs)+Sb | 23.6 (-3.9, 1.4) | 806.7 (-25.3, 98.9) | 4.5%
5th (K,Cs)+Sb | 24.9 (-17.2, 1.0) | 725.5 (-46.5, 24.6) | 4.9%
4th (K,Cs)+Sb | 14.5 (-2.1, 0.40) | 609.3 (-70.5, 9.5) | 3.7%
3rd (K,Cs)+Sb | 9.92 (-1.5, 1.5) | 489.09 (-6.8, 18.7) | 4.2%
2nd (K,Cs)+Sb | 9.73 (-0.30, 0.86) | 334.3 (-1.8, 2.1) | 1.7%
1st (K,Cs)+Sb | 9.22 (-2.9, 0.78) | 159.3 (-1.6, 0.9) | 1.2%
Sb | 5.2 (-0.11, 0.35) | 36.74 (-0.26, 0.13) | 
Substrate (MgO) | 1.5 (-, -) |  | 
XRR simulation result of K/Cs co-dep sample.
Colored solid lines: simulation; Open circle: measured data. Error noted is 5% of change in logarithm FOM function