## Slide 1: Operational Experience for High Power Spallation Targets
John Haines, Bernie Riemer (ORNL),
Masatoshi Futakawa (JAEA),
Werner Wagner and Michael Wohlmuther (PSI)
4th High Power Targetry Workshop
Malmö, Sweden
May 2, 2011

## Slide 2: MW-Class Spallation Targets
SINQ at the Paul Scherrer Institut (PSI)
SNS at the Oak Ridge National Laboratory (ORNL)
JSNS at the Japan Atomic Energy Agency (JAEA)

## Slide 3: SINQ experience

## Slide 4: SINQ Facility
SINQ Target Station
Target bulk shielding
Proton beam:
CW
590 MeV
~ 1.5 mA  0.9 MW

## Slide 5: Target Evolution at SINQ
2000 - 2009:SINQ-Target Mark 3:
Lead rods, with steel clad
42% increase in neutron yield
1997-1999: SINQ Target Mark 2
Water-cooled Zircaloy rods
Aug- Dec 2006: MEGAwatt Pilot Experiment:
Joint international initiative to design,
build, licence, operate and explore
a liquid metal spallation target
for 1 MW beam power

## Slide 6: MEGAPIE A liquid metal target for SINQ
MEGAwatt Pilot Experiment:
Lead-Bismuth-Eutectic (LBE, Tm=125oC)
Increase the neutron flux at SINQ
Demonstrate the feasibility of a liquid metal target for high-power spallation and ADS applications

## Slide 7: MEGAPIE (Pb-Bi) Target Features
target
head
electro-
magnetic
pumps
beam
window
heat
exchanger
safety
hull
lower target
assembly
central flow
guide tube

## Slide 8: MEGAPIE Target Operated Continuously for Four Months
First protons on target, August 14
First protons on target August 14, 2006
On beam: August 14 – December 21, 2006
Accumulated charge: 2.8 Ah
Peak Current: 1400 mA
Beam trips (< 1 min): 5500
Interrupts (< 8 h): 570
PIE will be discussed in Wagner presentation

## Slide 9: MEGAPIE Target Enhanced SINQ Neutron Flux
Fluxes measured by Au foil activation (in neutrons/cm2/s/mA)
 | SINQ 2005 | Err. (%) | MEGAPIE 2006 | Err. (%) | ratio
ICON | 3.80E+8 | ~5 | 6.89E+8 | ~5 | 1.81
NEUTRA | 2.59E+7 | ~5 | 4.80E+7 | ~5 | 1.85
EIGER | 6.46E+8 | ~5 | 1.04E+9 | ~5 | 1.61
NAA | 5.82E+12* | ~5 | 1.04E+13 | ~5 | 1.79

## Slide 10: Improvement options for the solid Pb canneloni target
Zr cladding (replacing steel)
compaction: closer rod-packing (2 mm gap  1.2 mm)
thinner tube wall (0.75 mm  0.5 mm)
Pb-reflectors filling the gap around the canneloni structure
inverted calotte of safety hull
No (or less) STIP samples
→ 10-13%
→ 5%
→ 5%
→ 10%
→ 5%
→ 10%
50%
Scetch from Knud Thomsen
predicted gain

## Slide 11
Status:
Operated @ 0.9 MW
April 2009 – Dec. 2010
The new Zr-Pb cannellomi target for SINQ
Neutron flux gain:
54% compared to Target Mark 3 (2004 / 2005)

## Slide 12: SINQ neutron production statistics 1997-2010
Together with 75% p-beam upgrade 300% more flux since 1999!!
MEGAPIE
compact cannelloni

## Slide 13: JSNS mercury target

## Slide 14
JSNS Hg Target
Proton Beam (design parameters):
  3 GeV, 25 Hz rep rate, 0.33 mA  1 MW
Hg Target:
  Cross-flow type, with multi wall vessel
  Hg leak detectors between walls
  All components of circulation system on trolley
  Hot cell : Hands-on maintenance
  Vibration measuring system to diagnose pressure wave effects
Length 12 m
Height 4 m
Width 2.6 m
Weight 315 ton

## Slide 15
Beam power on JSNS target

## Slide 16
Temperature rise of mercury vessel for 120 kW & 300 kW beam power agreed with estimates
  Confirmed operation of the mercury circulation system； EM pump, heat exchanger, etc.
Hg
Proton beam
Temp. measuring
point
Confirmation of target system design

## Slide 17: Bubble Injection Needed to Mitigate Cavitation Damage
A
B
C
A
B
Suppression against cavitation bubble by compressive pressure emitted from gas-bubble expansion.
C
3 mechanisms for each region
Center of thermal shock : A
Absorption
Propagation path : B
Attenuation
Negative pressure field : C
Suppression
Absorption
Attenuation
Suppression
Bubble<50 m

## Slide 18: Bubblers applicable to target
Venturi
Difficult to cont., D>50 m
High erosion risk
High pressure drop
Needle
Controllable, D>500 m,
Flow induced vibration, Erosion
Swirl
Controllable, D<50 m,
Acceptable pressure drop
He gas supply
What bubbler is the most suitable under mercury target condition ?

## Slide 19: Gas supply system for bubblers
Surge tank
Remove bubbles > 100 m
Heat exchanger and high points
Evaluate effects of remaining bubbles or gas layers on mercury flow
Gas supply system
Control gas pressure and flow rate
EM Pump
Mercury target
Bubbler
Heat
exchanger
Target trolley
Component tests are being carried out in water and mercury loops
Conceptual design is being made by a company
Mercury loop
EM pump
HX
Surge tank

## Slide 20: Strong Collaboration Between JSNS and SNS on Hg Target Development
Facilities for cavitation damage characterization and mitigation tests:
  Off-line tests
    JAEAs impact testing apparatus (MIMTM)
    ORNLs full-scale Hg loop (TTF)
  In-Beam Tests at LANLs WNR facility
Characterize bubbles, measure mitigation effects, etc.
WNR
TTF
MIMTM

## Slide 21: SNS mercury target

## Slide 22: SNS Mercury Target
SNS Ultimate Parameters
1 GeV protons
2 MW average beam power
Pulse duration ~ 0.7 s
60 Hz rep rate

## Slide 23: Mercury Loop Parameters @ 2 MW
Power absorbed in Hg 1.2 MW
Nom Op Pressure 0.3 MPa
Flow Rate 340 kg/s
Vmax (In Window) 3.5 m/s
Temperature
  Inlet to target 60ºC
  Exit from target 90ºC
Total Hg Inventory 1.4 m3
Centrifugal Pump Power 30 kW
SNS Hg Target operates at low temperature and pressure
Peak power density in mercury ~ 800 MW/m3

## Slide 24: Target Service Bay
Hg Pump
Carriage
Target Service Bay
  Stainless-steel lined
  4 window workstations
  8 through-the-wall manipulators
  7.5 ton crane
  Pedestal mounted manipulator
  Shielded transfer bay
7.5 Ton Crane
Dual Arm Telerob Manipulator on extended pedestal

## Slide 25: SNS Power Ramp-Up
Currently operating at ~ 1 MW
Target #1
Target #2
Target #3
Target #4
April 3:
End of life reached!

## Slide 26: Mercury Target Status
1st target module replaced July 2009; 2nd target replaced July 2010
  Both during planned extended maintenance periods
  Both exceeded original goal of 5 dpa (reaching almost 8 dpa)
Plans are still to run the next few targets to end-of-life, i.e. mercury leaks from primary container to its water-cooled shroud (or 10 dpa)
  If cavitation damage limits lifetime, will operate at a power level consistent with using four targets/year (~ 1250 hour lifetime)
Three spare target modules on-site; five more by 2012

## Slide 27: 3 April 2011: Target #3 reached an early end of life
Leak detectors in interstitial space between mercury vessel and shroud gave unanimous indications of a leak
Plan was to replace T3 during summer maintenance period
  It would have reached ca. 10 dpa by that time
Target replacement to be completed by 17 April
Investigation / PIE now under way
  Must locate and characterize the leak
  It is not confirmed that cavitation is the cause

## Slide 28: Mercury target module lifetime remains uncertain
1250 hours corresponds to goal of 4 target replacements/year
Demonstrated power limit is now > 900 kW

## Slide 29: Results of Post-Irradiation Examination of Hg Target Module #1
Inner surface of wall between bulk Hg and small channel
Target #1:
  Cavitation damage phenomenon confirmed on inner wall at center of target
  Outer wall fully intact; inner wall at off-center location shows little or no damage
  Damage region appears to correlate with regions of low Hg velocity, but not such a clear distinction on Target #2
60 mm

## Slide 30: Target #2 survived through planned operating period but inner wall suffered more damage
Bulk Hg Flow Surface - UNCLEANED
Horizontal operating orientation

## Slide 31: Hg Target Development Plans
New mercury laboratory now operational in SNS Experiment Hall
Continue to pursue gas injection schemes for mitigating cavitation damage
  Gas injection looks promising, but work remains to optimize and implement
    Small gas bubbles and/or gas curtain near wall
    Collaborating with JAEA, RAL, and several university and industrial partners
More detailed PIE of samples from first two three spent target modules will be conducted

## Slide 32: Target Imaging System
Implemented Target Imaging System on second target
  System was functional for full life of 2nd target (3200 MW-h)
  3rd target installed with enlarged and improved coating pattern
  Improved resolution system was installed with 3rd Proton Beam Window in December 2010
Target Imaging System
Flame Sprayed 0.25 mm thick coating (Al2O3+ 1.5% CrO)
200mm x 70 mm pattern

## Slide 33: Concluding Remarks
MEGAPIE, SNS, and JSNS projects successfully implemented liquid metal targets designed for ~ 1 MW
  MEGAPIE experiment completed in 2006; demonstrated ~ 1 MW reliable operation
  SNS operating reliably at 1 MW; 3rd target end of life; ramp-up to 1.4 MW may be impacted
  JSNS was operating reliably at 220 kW; plan to ultimately achieve 1 MW
SINQ is pursuing more optimal solid targets
  Liquid metal target is not being pursued in view of cost and effort, and because the neutron flux of new solid targets is within 15% of MEGAPIE
  Next generation Pb-Bi target (LIMETS) being pursued as an experiment
Cavitation damage remains a concern for pulsed sources with liquid metal targets
  Target lifetime uncertain but reasonably long lifetime established for SNS at 1 MW
    Cause of target 3 end 0f life not yet determined; ultimate power / lifetime limit remains to be discovered
  Strong R&D collaboration between SNS and JSNS
Future projects considering target alternatives
  SINQ upgrades, CSNS, ESS, SNS-STS, MTS
  Both liquid and solid target options under consideration